Reduction of Carbonization and Gas Emissions using Mechatronics based Intelligent Laser Beam Machining for cutting Leather with better Environmental measures for Operator Health

Vasanth Swaminathan1, Muthuramalingam Thangaraj2

1,2 Department of Mechatronics Engineering

College of Engineering and Technology, SRM Institute of Science and Technology

SRM Nagar, Kattankulathur – 603203, Tamilnadu, India

vasanths@srmist.edu.in

Abstract

Laser cutting is gaining considerable attention for leather cutting, since it can eliminate the need for certain manual procedures. The attributes of laser technology for leather cutting include adaptability, mass production, the capability to cut complicated patterns, the ease of producing tailored components, and a reduction in leather waste. Due to the thermal influence of conventional laser cutting, a slight carbonization of the cut edge occurs. In this investigation, an endeavour is proposed to design and develop a self-tuned laser diode assisted laser beam machining system using a mechatronics engineering approach to analyse the impacts of the laser diode on environmental measures such as carbonization, striations, dross, and emission formation in leather cutting. It has been inferred that only little effort was made on the laser diode assisted LBM process to reduce carbonization and gas emissions. This machining system has a wide range of Pulse Width Modulation (PWM) control, self-tuned Standoff Distance (SOD) control, effective emission filters, and Graphical User Interface (GUI) implementation with a touch display. The chrome vegetable tanned cow leather was machined under various machined conditions. The analysis of carbonization through machine vision, kerf width, Material Removal Rate (MRR), and emission rate has been analysed and recorded to obtain the optimal control loop approach and optimal parameters for leather cutting.

keywords: Laser Diode; PWM; SOD; Carbonization

Introduction

Laser cutting is a technology used in many engineering sectors. Its effectiveness depends on several factors, such as laser wavelength, power density, scan speed, absorptivity, thermal diffusivity, and boundary constraints [1]. Leather cutting in industry is the process of forming leather into various shapes and sizes that are used to create a range of leather goods. It involves using special tools and techniques to accurately cut and shape the leather into the desired shape. It is a skilled craft that requires precision and accuracy to ensure that the leather products are of the highest quality. Leather cutting machines are used in the leather industry to create precise and consistent cuts in leather materials. These machines are often computer-controlled, allowing for a greater level of accuracy and efficiency than manual cutting. They can be used for a wide variety of leather goods, including clothing, furniture, bags, and shoes. Laser technology is now commonly used in industrial operations to ensure consistent quality and can produce complicated geometries, individual designs, prototypes, and small-scale goods. Laser cutting is a very efficient and accurate material cutting technology. It excels in producing products of superior quality quickly while subjecting the equipment to minimal wear and tear. Additionally, it eliminates the need for specialized tools, such as design marks and dies, and reduces storage and disposal costs associated with traditional cutting methods [2]. LBM is widely used for its high ablation rate, excellent surface finish, and the ability to control material removal rate by adjusting pulse frequency [3]. Maintaining a constant level of quality is critical in industrial processes, and laser technology is well-suited to achieve this goal. When laser cutting settings are properly selected, it produces consistently exact cuts. Furthermore, in terms of geometry, laser technology is very flexible and it can create intricate geometries, unique patterns, prototypes, and small-scale products [4]. Modern laser cutting machines are highly advanced pieces of technology that are capable of cutting various types of materials of different thicknesses and surface finishes. They are equipped with sophisticated process parameters, real-time monitoring and control systems that allow for adjustments to be made in order to achieve the best possible cut quality [5]. Laser diodes have certain intriguing characteristics that make them attractive candidates for usage in numerous practical applications, such as low cost, small size, great reliability and relative ease of operation [6, 7].

Experimental investigations of LBM have revealed the process input factors such as cutting depth, optical power, cutting material shape and size, assist gas type and mode of operation affect process performance [8]. Increasing the laser power and the pulse frequency could improve the machining efficiency. It was also found that the peak surface temperature increased with increasing laser power and pulse frequency. The parameters of laser power, scanning speed and pulse frequency should be carefully considered to optimize the machining performance [9]. Laser processing is a highly efficient and precise method of machining due to its non-contact and no tool wear properties. It offers great accuracy and surface finish with minimal material waste, as well as high machining flexibility. However, there is a potential for defects such as HAZ [10]. In the leather manufacturing, hides of buffalo and cow, skins of goat and sheep are the most often and broadly used permitted sources. SEM (Scanning Electron Microscope) images of buffalo and cow hides, skins of goat and sheep reveal their unique leather compositions and textures. The spectra of leather samples recorded directly on the surface was exploited using Fourier Transform Infrared (FTIR) spectroscopy [11].Peak power, pulse power, pulse repetition rate, pulse width, and wavelength are the most significant solid state pulsed laser performance parameters. The major features are the beam quality and optical power, along with the compact design [12]. Surface morphology is crucial in the machining industry because it influences the visual appearance as well as the operating performance characteristics of diverse end products [13]. Pulsed laser beam machining is an efficient and accurate way to achieve high-quality cuts [14]. Laser cutting may produce potentially hazardous byproducts such as fumes, small particles, and Volatile Organic Compounds (VOCs). Household Manufacturing Equipment (HME) is a new source of air pollution, and studies have found contaminants including sulphur and barium in the particles emitted during leather processing. Lowering the laser power is an efficient way to reduce the emission of both particle and gaseous pollutants from these equipment [15].

Based on the extensive review of the literature, it became clear that the use of self-tuned laser diode technology for leather cutting has received little attention. There was an obvious lack of reported control strategies for these processes. Consequently, this study sought to develop a self-tuned laser diode-assisted laser beam machining system with the objective of enhancing process performance.

2. Material and Methods

The block diagram in Figure 1 illustrates the complete system, including the microcontroller units, measurement sensors, actuation drivers, stepper motors, and the laser module. The blue laser diode with 5.5W optical power needs 12V and 2A current inputs. The laser diode driver unit controls laser irradiation.

Figure 1 (a) Block diagram of laser diode assisted LBM (b) PWM signal generated by ESP 32 (c) Experimental Setup

The stepper motor driving the Z-axis of the laser diode machining system, which controls the standoff distance, is supplied with power by the Power Supply Unit. The Raspberry Pi equipped with all hardware and sensor systems features an LCD display that provides touch-based interaction [16,17]. The Raspberry Pi is pre-configured with the Open Builds CAM software, enabling precise control at each phase of the process. The connection has been established between the Raspberry Pi and the Arduino UNO microcontroller [18]. Based on the observed distance, it is used to regulate the vertical axis with the support of the Time-of-Flight sensor.

2.1 Need for control approaches in laser diode LBM

The existing LBM configuration does not have a control mechanism that allows users to customise and attain an ideal leather cutting process. Comparative tests were conducted in order to ascertain the optimal control loop method and appropriate parameters for leather cutting. The leather samples were subjected to cutting using a 20W laser diode, employing both open-loop and closed-loop SOD mechanisms [19]. They are classified as SOD control in open loop configuration and SOD control in closed loop configuration.

Figure 2 SOD control in open loop configuration

Figure 3 SOD Control in closed loop configuration

Figure 2 shows the SOD control in open loop configuration. The open-loop SOD control was executed at three distinct levels: 18mm, 20mm, and 22mm, assisted by software, utilizing a Vernier calliper. The predefined distance is ascertained after positioning the leather within the work center, and it is calculated using a Vernier calliper. This measurement is subsequently input into the CNC software, which commands the GRBL controller to adjust the Z-axis responsible for holding the laser during the cutting process. Closed-loop SOD control, illustrated in Figure 3, involves the utilization of an Arduino Uno microcontroller to regulate the SOD based on the specified distance, achieved through the Time-of-Flight sensor. The ToF sensor functions as a measuring device that eliminates the need for manual distance adjustment. An exceptional benefit of employing this control loop methodology is that it maintains a consistent SOD, even when dealing with an uneven leather surface, all while eliminating any human intervention.

2.2 Design of experiments

The investigations were conducted with chrome vegetable-tanned cow leather of 1 mm thickness, chosen for its adaptability to a variety of applications. The selection of a circular shape with a diameter of 30 mm was based on its intrinsic geometric properties. This study emphasises the significance of selecting an Orthogonal Array (OA) for experimental design while using the Taguchi technique in performing experiments [20].

Table 1 L9 orthogonal array based design of experiments

| Sl.No | Parameters | Units | Level 1 | Level 2 | Level 3 |
| --- | --- | --- | --- | --- | --- |
| 1. | SOD | mm | 18 | 20 | 22 |
| 2. | Feedrate | mm/min | 200 | 250 | 300 |
| 3. | Duty Cycle | % | 70 | 75 | 80 |

Table 2 Experimental trial in the proposed study

| Experimental Trial | SOD (mm) | Feedrate (mm/min) | Duty Cycle (%) |
| --- | --- | --- | --- |
| 1 | 18 | 200 | 70 |
| 2 | 18 | 250 | 75 |
| 3 | 18 | 300 | 80 |
| 4 | 20 | 200 | 75 |
| 5 | 20 | 250 | 80 |
| 6 | 20 | 300 | 70 |
| 7 | 22 | 200 | 80 |
| 8 | 22 | 250 | 70 |
| 9 | 22 | 300 | 75 |

The present investigation used the L9 orthogonal array for conducting experiments in the laser beam machining process, since it included three input factors. Table 2 illustrates the experimental design using the L9 orthogonal array.

3 Results and Discussion

The leather specimens have been machined using the proposed laser diode assisted cutting process. Figure 4 shows the Surface morphology analysis of machined leather specimens acquired by the scanning electron microscope (SEM). From the composition analysis, it was observed that the carbon particles have been available in considerable amount over the top layer of the machined leather specimen. That is why the carbonization layer is clearly visible over the SEM image. The heat affected zone is also visible as white layer zone and region. The less striation marks have been available due to the lower power density created by the laser diode assisted cutting process. However, the carbonization layer needs to be quantified for the analysis purposes.

Figure 4 Surface morphology analysis of machined leather specimens

Digital microscope is an advanced optical instrument used to focus on the leather surface and zoom into get a clear view of the cross section of experimented leather samples. The image obtained from digital microscope undergoes processing via a Python program, which provides the results in terms of carbonization extent and displays the outcomes as both a percentage and a pixel count. OpenCV and NumPy are the two essential libraries used in the process of converting an RGB image to binary image using OpenCV in python.

Figure 5 Procedure for converting acquired image to binarized image

The procedure for converting acquired image to binarized image is shown in Figure 5. For determining the black and white portions of a grayscale image, a threshold value is used. The threshold function is used to apply this threshold, which changes pixel intensities that are higher than or equal to the threshold into white (255), and those that are below it into black (0).

The equation to compute the percentage of black pixels can be formulated as

Percentage of black pixels=Black Pixels CountTotal Pixels Count*100                                                (1)

3.1 Performance analysis of carbonisation in SOD control of open loop and closed loop configurations

Table 3 presents the carbonization percentage results for a process utilizing SOD control. In the case of open loop SOD control, the average carbonization percentage lies between 50% and 60%. The average carbonization percentage for closed loop SOD control ranges from 49% to 51%.

Table 3  Carbonization of the process using open loop and closed loop SOD control

| Trial No | SOD (mm) | FR (mm/min) | DC (%) | Carbonization (%) |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | Open loop SOD control | Closed loop SOD control |
| 1 | 18 | 200 | 70 | 56.14 | 54.54 |
| 2 | 18 | 250 | 75 | 58.29 | 56.68 |
| 3 | 18 | 300 | 80 | 58.10 | 56.30 |
| 4 | 20 | 200 | 75 | 54.11 | 51.54 |
| 5 | 20 | 250 | 80 | 51.53 | 50.75 |
| 6 | 20 | 300 | 70 | 60.07 | 51.49 |
| 7 | 22 | 200 | 80 | 54.03 | 49.47 |
| 8 | 22 | 250 | 70 | 59.34 | 51.09 |
| 9 | 22 | 300 | 75 | 50.42 | 49.72 |

As per photometric Inverse square law, the irradiance is indirectly proportional to the square of distance between source tip and specimen i.e., SOD. Since the power density can control the carbonization effectively, the SOD can efficiently modify the carbonization region. The formula for inverse-square law is given as

I α 1d2                                                                                  	                 (2)

where, d is the distance & I is radiation intensity

The SOD may change during the cutting process owing to the change in specimen random thickness and feed rate of actuator constraints. The closed loop control of any parameter can enhance the accuracy of reaching set point efficiently. Since the closed loop SOD control has the adaptability on maintaining the constant with respect to thickness and distance, it could produce lower carbonization.

Figure 6 Comparison of carbonization on SOD control in open loop and closed loop configuration

Figure 6 provides a graphical comparison between software-assisted open loop and closed loop SOD control. The illustration suggests that implementing a closed control loop for SOD reduces carbonization during the leather cutting process. On the basis of the graphical representation, it is conceivable to figure out that closed loop SOD control is more appropriate for precise leather cutting.

3.2 Performance Analysis on Emission Rate in Open Loop and Closed Loop SOD Control

Table 4 displays the measured emission rates in parts per million (ppm) for both interior and exterior values in open loop SOD and closed loop SOD control. These measurements were obtained using the SCD30 sensor, which was positioned both inside and outside the laser diode-based LBM. Notably, the interior emission rates in ppm were recorded without any filtration process, whereas the exterior emission rates in ppm were measured with the application of a customized filtration process.

Table 4 Emission rate of the process using open loop SOD control

| Trial No | SOD (mm) | FR (mm/min) | DC(%) | Emission Rate (ppm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Open loop SOD Control |  |  | Closed loop SOD Control |  |  |
|  |  |  |  | Interior (I) | Exterior (E) | I-E (ppm) | Interior (I) | Exterior (E) | I-E (ppm) |
| 1 | 18 | 200 | 70 | 551.11 | 478.81 | 72.30 | 555.28 | 466.74 | 88.54 |
| 2 | 18 | 250 | 75 | 560.18 | 476.00 | 84.18 | 545.99 | 455.43 | 90.56 |
| 3 | 18 | 300 | 80 | 541.82 | 459.89 | 81.93 | 556.98 | 469.94 | 87.04 |
| 4 | 20 | 200 | 75 | 543.83 | 461.28 | 82.55 | 542.09 | 448.37 | 93.72 |
| 5 | 20 | 250 | 80 | 533.25 | 443.99 | 89.26 | 544.03 | 450.35 | 93.68 |
| 6 | 20 | 300 | 70 | 557.53 | 474.28 | 83.25 | 549.24 | 464.67 | 84.57 |
| 7 | 22 | 200 | 80 | 557.54 | 474.65 | 82.90 | 549.79 | 463.99 | 85.80 |
| 8 | 22 | 250 | 70 | 534.78 | 451.31 | 83.47 | 545.20 | 450.90 | 94.30 |
| 9 | 22 | 300 | 75 | 534.83 | 446.64 | 88.19 | 540.14 | 449.51 | 90.64 |

From Table 4 the average emission rate in ppm has a higher emission rate difference of 89.26 ppm and lower emission rate difference of 72.30 ppm for open loop SOD control. For closed loop SOD control the average emission rate in ppm has a higher emission rate difference of 94.30 ppm and lower emission rate difference of 84.57 ppm.

Figure 7 Comparison of Emission rate on SOD control in open loop and closed loop configuration

Figure 7 illustrates comparing open and closed loop SOD control for leather machining. It has been found that closed-loop SOD control is more effective for emissions management. This enhanced emission control is attributable to the closed control loop applied to SOD parameters and the use of a customised filtration procedure during the release of pollutants into the environment.

4. Conclusion

The present study investigated the effects of Stand Off Distance (SOD) on the carbonization of leather and emission rate. This was achieved by using a Laser Beam Machining (LBM) technique that used a laser diode. The results of a comprehensive investigation involving experiments, measurements, and observations indicate that,

- The implementation of SOD in a closed-loop configuration resulted in a significant reduction in carbonization, lies between 49% to 51%.

- The SOD control in closed loop configuration has an efficient emission rate lies between 94.30 ppm to 84.57 ppm due to the implementation of control loop on SOD parameters and utilizing filtration process while emitting the fumes in the environment.

5. Acknowledgements

The authors would like to acknowledge and thank the IULTCS for funding the proposed study to achieve the enhanced laser beam machining process on cutting leather materials.

6. References

- Elsheikh, A.H., Shanmugan, S., Muthuramalingam, T., Kumar, R., Essa, F.A. and Mahmoud Ibrahim, A.M., Modeling of the Transient Temperature Field during Laser Heating, Lasers in Manufacturing and Materials Processing, 8, 97-112, 2021.

- Stepanov, A., Manninen, M., Parnanen, I., Hirvimaki, M. and Salminen, A., Laser cutting of leather: tool for industry or designers?, Physics Procedia, 78, 157-162, 2015.

- Muthuramalingam, T., Moiduddin, K., Akash, R., Krishnan, S.,Hammad Mian, S., Ameen, W. and Alkhalefah, H., Influence of process parameters on dimensional accuracy of machined Titanium (Ti-6Al-4V) alloy in Laser Beam Machining Process, Optics & Laser Technology, 132, 106494, 2020.

- Khoshaim, A.B., Elsheikh, A.H., Moustafa, E.B. et al., Experimental investigation on laser cutting of PMMA sheets: Effects of process factors on kerf characteristics, Journal of Materials Research and Technology, 11, 235-246, 2021.

- Levichev, N., Tomas Garcia, A., Kardan, M., Cattrysse, D. and R.Duflou, J., Experimental validation of a machine learning algorithm for roughness quantification in laser cutting, Procedia CIRP, 113, 564-569, 2022.

- Nasim, H. and Jamil, Y., Diode lasers: From laboratory to industry, Optics & Laser Technology, 56, 211-222, 2014.

- Rodrigues, G.C., Vanhove, H. and Duflou, J.R., Direct diode lasers for industrial laser cutting: a performance comparison with conventional fiber and CO2 technologies, Physics Procedia, 56, 901-908, 2014.

- Dubey, A.K. and Yadava, V., Laser beam machining – A review, International Journal of Machine Tools and Manufacture, 48, 609-628, 2008.

- Guo, Y., Yang, X., Kang, J., Li, M., Xie, Q., Xiao, J. and Zhang W.,  Experimental investigations on the laser-assisted machining of single crystal Si for optimal machining,141,107113, 2021.

- Chen, L., Huang, Y., Li, W., Yang, R., Chen, X., Zhang, G. and Rong, Y., Acoustic emission monitoring and heat-affected zone evaluation of CFRP laser cutting, Composite Structures, 304, 116419, 2023.

- Varghese, A., Jain, S., Amalin Prince, A. and Jawahar, M., Digital microscope image sensing and processing for leather species identification, IEEE Sensors Journal, 20, 10045-10056, 2020.

- Johan Meijer., Laser beam machining (LBM), state of the art and new opportunities, Journal of Materials Processing Technology, 149, 2-17, 2004.

- Gisario, A., Boschetto, A. and Veniali, F., Surface transformation of AISI 304 stainless steel by high power diode laser, Optics and Lasers in Engineering, 49, 41-51, 2011.

- Nur Rohman, M., Rong Ho, J., Cheng Tung., Ping Tusi, H. and Kuang lin, C., Prediction and optimization of geometrical quality for pulsed laser cutting of non-oriented electrical steel sheet, Optics & Laser Technology, 149, 107847, 2022.

- Sik ko, H., Bin Jeong, S., Phyo, S., Lee, J. and Hee Jung, J., Emission of particulate and gaseous pollutants from household laser processing machine, Journal of Environmental Sciences, 103, 148-156, 2021.

- Vasanth, S., Muthuramalingam, T.,  Prakash, S.S., Raghav, S.S., Logeshwaran, G., Experimental investigation of PWM laser standoff distance control for power diode based LBM, Optics & Laser Technology, 158, 108916, 2023.

- Vasanth, S., Muthuramalingam, T., Prakash, S.S., Raghav, S.S., Logeshwaran, G., Implementation and performance analysis of combined SOD and PWM control in diode based laser beam machining process on leather specimen, Optics & Laser Technology, 169, 110093, 2024.

- Vasanth, S.; Muthuramalingam, T. Application of laser power diode on leather cutting and optimization for better environmental quality measures, Archives of Civil and Mechanical Engineering, 21, 54, 2021.

- Vasanth, S.; Muthuramalingam, T.; Prakash, S.S.; Raghav, S.S., Investigation of SOD control on leather carbonization in diode laser cutting, Materials and Manufacturing Processes, 38,  544-553, 2022.

- Vasanth, S.; Muthuramalingam, T., Measurement of carbonization region on leather cutting in CO2 and diode laser-based laser beam process, Proceedings of the Institution of Mechanical Engineers, Part E: Journal of Process Mechanical Engineering, 236, 1076- 1082, 2022.