Carbon Quantum Dots Derived from Leather Solid Waste: A Novel, Efficient and Sustainable Masking Agent for Leather Tanning

Xin Shi1, 2, Siqi Liu1, 2, Haibin Gu1, 2*

1 Key Laboratory of Leather Chemistry and Engineering of Ministry of Education, Sichuan University, Chengdu, Sichuan, China

2 National Engineering Laboratory for Clean Technology of Leather Manufacture, Sichuan University, Chengdu, Sichuan, China

Corresponding author: Haibin Gu, e-mail: guhaibinkong@126.com

Abstract

Tanning is a key industrial process in leather production and a crucial step in transforming skin (or hide) into leather. Traditional chrome tanning possesses troubling application prospects due to its pollution problem. Chrome-free metal tanning agents (such as Zr (IV) and Al (III)) are widely recognized for their strong coordination ability and environmental friendliness, which could replace chrome tanning to achieve efficient and sustainable tanning. However, the strong crosslinking reactions of these metal tanning agents with leather surface fibers could greatly weaken their uniform penetration ability inside the leather, thereby affecting their tanning performance. Therefore, the development of masking agents plays a crucial role in improving the tanning performance of these chrome-free metal tanning agents. Carbon quantum dots (CQDs), as a new type of carbon nanomaterials, have outstanding characteristics such as easy surface modification, excellent chemical stability, and biocompatibility, and have considerable application prospects in many fields. Herein, we synthesized biomass-derived functionally modified carbon quantum dots (BFM-CQDs) by the typical but simple hydrothermal method, in which the delimed cattle hide waste (DCHW) was applied as the synthetic precursor and carboxyl/phenolic hydroxyl reagents were added to achieve functional modification of BFM-CQDs. The resulting BFM-CQDs had rich coordination groups on their surface, which could form the coordination interactions with the chrome-free metal tanning agents during the tanning process, thus weaken their crosslinking reactions with collagen fibers on the leather surface, promoting uniform penetration and efficient binding of tanning agents, and thereby enhancing the tanning effect. Results indicate that BFM-CQDs, as the masking agents, could effectively improve the shrinkage temperature of leather and modify the tanning effect of chrome-free metal tanning agents. In short, this work not only provides a new type of CQDs prepared by using the leather solid waste, which realizes the high value-added resource utilization of leather solid waste, but also contributes to a novel strategy for efficient and sustainable tanning by using the CQDs as masking agents.

Keywords: Leather solid waste; Carbon quantum dots; Tanning; Masking agent

- Introduction

Leather making is a traditional industry with a long history, which is a technological industry that transforms the byproduct of animal husbandry - raw skin - into leather, perfectly reflecting the idea of "transforming decay into magic". Tanning, as an important step in the leather making process, is also the key to converting raw leather into leather1. Traditional tanning is usually dominated by chrome tanning, which has excellent tanning performance, but at the same time, it brings prominent environmental issues such as chromium pollution2. Aluminum tanning and zirconium tanning, with their excellent tanning performance and environmental friendliness, are considered the most promising new chrome-free tanning technologies to replace chrome tanning3. However, aluminum tanning agents and zirconium tanning agents have a strong cross-linking effect with the surface of skin collagen, making it difficult to penetrate into the skin during the tanning process, leading to insufficient penetration and reducing the tanning performance of the tanning agent4. The masking agent, with its coordination effect with chrome free metal tanning agents, can effectively weaken the crosslinking effect between the tanning agent and skin collagen during the tanning process, thereby allowing for more thorough penetration, and is widely used in chrome-free metal tanning technology5.

Carbon quantum dots (CQDs) are a new type of carbon-based nanomaterials with excellent biocompatibility, biodegradability, conductivity, photoluminescence, and easy chemical modification 6. They are widely used in technical fields such as biosensing, biological imaging, and light-emitting devices7. In recent years, the preparation of carbon quantum dots using biomass as a precursor has received widespread attention8. Biomass-derived carbon quantum dots (BFM-CQDs) can not only achieve high value-added conversion and utilization of biomass resources, but also have ecological value and environmental significance.

During the leather making process, a lot of solid waste is generated, including raw hide trimming waste before tanning, waste non collagen components, removed hair, and leather waste after tanning 8. In our work, we use pre tanning waste in the leather industry - limed cattle hide waste as the carbon source, and after deashing treatment, we obtain the delimed cattle hide waste (DCHW). This is used as a synthetic precursor, and modification reagents are added to obtain a biomass-based functional modified carbon quantum dots (BFM-CQDs) solution through hydrothermal reaction. Using new carbon quantum dots as masking agents for chrome-free metal tanning agents, by modifying the surface groups of carbon quantum dots with biomass-based functionalities, the masking effect of chromium free metal tanning agents is weakened, weakening the interaction between tanning agents and the surface of skin collagen, resulting in more complete and uniform penetration, achieving green, efficient, and sustainable tanning technology (Figure 1).

Figure 1. Schematic diagram of the possible mechanism of action of BFM-CQDs masking agent in chrome-free metal binding tanning

- Material and Methods

2.1 Materials

Limed cattle hide waste and picked goat hides were purchased from Qingyang Century Fur Co., Ltd. (Chengdu, China). Anhydrous citric acid is provided by Kelong Chemical Reagent Factory (Chengdu, China). Sodium alginate and octahydrate aluminum sulfate compounds were purchased from Cologne Chemicals Co., Ltd. (Chengdu, China). Itaconic acid and zirconium sulfate tetrahydrate compounds are produced by Titan Technology Co., Ltd. (Shanghai, China). Sodium chloride was purchased from Jinshan Chemical Reagent Co., Ltd. (Chengdu, China). All reagents were analytically pure grades.

2.2 The synthesis of BFM-CQDs

The preparation process diagram is shown in Figure 2. Firstly, pretreat the solid waste of limed cattlehide: wash it with deionized water, cut it into small pieces, weigh it (based on this, denoted as m), add 500% m deionized water and 50% m ammonium sulfate by mass, and stir for 2 hours to obtain the delimed cattlehide.

Weigh 3 g of delimed cattlehide, measure 60ml of deionized water, load it into a polytetrafluoroethylene lining, transfer it to a high-temperature reaction kettle, react at 180 ℃ for eight hours, and centrifuge filter to obtain delimed cattlehide carbon quantum dots (DCH-CQDs/DCQDs). Similarly, by adding 0.1 g of modified reagents citric acid, alginate, and itaconic acid to the system, CA-DCH-CQDs (CCQDs), SA-DCH-CQDs (SCQDs), and IA-DCH-CQDs (ICQDs) can be prepared, respectively.

Figure 2. Synthesis schematic diagram of BFM-CQDs

2.3 Tanning process

The tanning process is shown in Tables 1-3, modified and optimized based on relevant literatures9, 10.

Table 1

Zirconium tanning process

| Process | chemical | quantity/% | duration/min | Temperature/C | pH | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| pickling | water | 100 |  |  |  |  |
|  | NaCl | 8 | 15 | 25 |  |  |
|  | formic acid | 0.8-1 | 15*3+30 |  | 3.0 | 1:10 dilution |
| tanning | Zirconium | 10 | 240 | 25 |  |  |
| basification | NaHCO3 | 1-1.5 | 5*20+40 |  | 3.8-4.0 | 1:20 dilution |
|  | water | 100 | 120 | 40 |  |  |

Table2

Aluminum tanning process

| Process | chemical | quantity/% | duration/min | Temperature/C | pH | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| pickling | water | 100 |  |  |  |  |
|  | NaCl | 8 | 15 | 25 |  |  |
|  | formic acid | 0.8-1 | 15*3+30 |  | 2.5 | 1:10 dilution |
| tanning | Aluminum | 10 | 240 | 25 |  |  |
| basification | NaHCO3 | 1-1.5 | 5*20+40 |  | 3.8-4.0 | 1:20 dilution |
|  | water | 100 | 120 | 40 |  |  |

Table3

Combination tanning process

| Process | chemical | quantity/% | duration/min | Temperature/C | pH | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| depickling | water | 100 |  |  |  |  |
|  | NaCl | 8 | 15 | 25 |  |  |
|  | NaHCO3 | 1-2 | 5*30+30 |  | 6.5 | 1:20 dilution |
| tanning | BFM-CQDs | 20 | 240 | 25 |  | liquid |
|  | formic acid | 0.8-1 | 15*3+30 |  | 3.0 | 1:10 dilution |
|  | Zirconium/ Aluminum | 10 | 240 | 25 |  |  |
| basification | NaHCO3 | 1-1.5 | 5*20+40 |  | 3.8-4.0 | 1:20 dilution |
|  | water | 100 | 120 | 40 |  |  |

2.4 Characterization

Observing the color and fluorescence of four carbon quantum dot solutions under visible light and ultraviolet light (365nm); Measure the photoluminescence spectrum of carbon quantum dot solution at a wavelength of 240-700nm using a fluorescence spectrometer (Hitachi F7100, Japan) with a slit of 5nm; Measure the photoluminescence spectrum of leather at a wavelength of 240-700nm using a fluorescence spectrometer (Hitachi F7100, Japan) with a slit of 2.5nm; Measure the shrinkage temperature of leather using a leather shrinkage temperature tester (Sunshine Electronics Research Institute, Shaanxi University of Science and Technology) (leather samples are measured in a 7% mass fraction sodium chloride solution); Obtain the thickness of various types of leather using a thickness gauge, and calculate the thickening rate using the formula A=(a0-a) /a*100% (A: thickening rate of leather sample (%), a: thickness of dried and pickled goat hide (mm), a0: thickness of tanned leather (mm)).

- Results and Discussion

As shown in Figure 3(a), the colors of DCQDs/CCQDs/SDCQs/ICQDs under visible light are light yellow, yellow, brown, and light yellow, respectively, and they exhibit blue fluorescence under 365nm ultraviolet light. In Figure 3(b), we found that the optimal emission peak of DCQDs at the excitation wavelength of 400nm is located near 465nm; In Figure 3(c), we can see that the optimal emission peak of CCQDs at the excitation wavelength of 440nm is located near 500nm; In Figure 3(d), we can see that the optimal emission peak of SCQDs at the excitation wavelength of 500nm is located near 540nm; In Figure 3(e), we can see that the optimal emission peak of ICQDs at the excitation wavelength of 380nm is located near 460nm.

According to the measurement results of shrinkage temperature (Figure 4 (a) and Figure 4 (c)), it can be seen that the leather shrinkage temperatures for pickling, zirconium tanning, zirconium/DCQDs combined tanning, zirconium/CCQDs combined tanning, zirconium/SCQDs combined tanning, and zirconium/ICQDs combined tanning are 64.7 ℃, 85.6 ℃, 95.6 ℃, 90.6 ℃, 91.8 ℃, and 93.1 ℃, respectively. The leather shrinkage temperatures for pickling, aluminum tanning, aluminum/DCQDs combined tanning, aluminum/CCQDs combined tanning, aluminum/SCQDs combined tanning, and aluminum/ICQDs combined tanning are 63.8 ℃ and 72.8 ℃, respectively 83.9 ℃, 80.6 ℃, 81.2 ℃, 82.4 ℃. Compared to pure zirconium tanning/aluminum tanning, the combination of BFM-CQDs tanning significantly increases the shrinkage temperature of leather. According to the measurement results of leather thickening rate (Figure 4 (b) and Figure 4 (d)), compared to pickled leather, the leather thickening rates of zirconium tanning, zirconium/DCQDs combined tanning, zirconium/CCQDs combined tanning, zirconium/SCQDs combined tanning, and zirconium/ICQDs combined tanning are 15.38%, 70.51%, 58.97%, 60.48%, and 62.82%, respectively. The leather thickening rates of aluminum tanning, aluminum/DCQDs combined tanning, aluminum/CCQDs combined tanning, aluminum/SCQDs combined tanning, and aluminum/ICQDs combined tanning are 6.56%, 67.2%, and 36.1%, respectively. 55.7% 62.3%. Compared to pure zirconium tanning/aluminum tanning, the combination of BFM-CQDs significantly improves the tanned thickness of leather, and the thickening rate corresponds to the shrinkage temperature, and tanning systems with higher shrinkage temperatures have higher thickening rates.

Figure 3. (a) shows the physical image of carbon quantum dot solution under visible light and 365nm ultraviolet light; (b) (c) (d) (e) are the PL spectra of DCQDs, CCQDs, SCQDs, and ICQDs, respectively.

Figure 4. (a) (c) show the shrinkage temperature results of different tanning methods for zirconium tanning system and aluminum tanning system, respectively; (b) (d) show the thickening rate results of different tanning methods for zirconium tanning system and aluminum tanning system, respectively.

- Conclusion

In this work, we have achieved the resource conversion and utilization of solid leather waste, and synthesized a new type of biomass based functional modified carbon quantum dots using deinked cowhide waste as a synthetic precursor through hydrothermal synthesis. With the advantages of carbon quantum dot materials (easy to synthesize, easy to modify, green and environmentally friendly), we have innovatively used them as a new type of masking agent in the leather tanning process to solve the difficulty of penetration in the chrome free metal tanning process Insufficient problem, achieving efficient, green, and sustainable tanning. From the measurement results of shrinkage temperature (increased by 7 ℃-11 ℃) and leather thickening rate (increased by 30% -60%), it can be seen that this new masking agent has a significant masking effect in the chrome free metal tanning process. The work of this project is still being further improved, and the specific confinement mechanism needs to be further explored. However, based on the current experimental results, we have successfully explored a new path for the preparation of biomass-based masking agents for chrome free metal tanning, which is expected to inject new development momentum into the resource utilization of waste biomass and efficient green tanning.

- Acknowledgements

This work was supported by the National Natural Science Foundation of China (21978180). Thank you for the support of the 2023 National College Student Innovation and Entrepreneurship Training Program of Sichuan University (project number: C2023124125).

- References

1. He X, Huang Y W, Xiao H Z, et al, Tanning agent free leather making enabled by the dispersity of collagen fibers combined with superhydrophobic coating, Green Chem., 23, 3581–3587, 2021.

2. Chen J, Ma J Z, Fan Q Q, et al, An eco-friendly metal-less tanning process: Zr-based metal-organic frameworks as novel chrome-free tanning agent, Journal of Cleaner Production, 382, 135263, 2023.

3. Jiang Z C, Xu S G, Ding W, et al, Advanced masking agent for leather tanning from stepwise degradation and oxidation of cellulose, Green Chem., 23, 4044, 2021.

4. Jiang Z C, Gao M, Ding W, et al, Selective degradation and oxidation of hemicellulose in corncob to oligosaccharides: From biomass into masking agent for sustainable leather tanning, Journal of Hazardous Materials, 413, 125425, 2021.

5. Ding W, Remón J, Gao M, et al, A novel synergistic covalence and complexation bridging strategy based on multi-functional biomass-derived aldehydes and Al (III) for engineering high-quality eco-leather, Science of the Total Environment, 862, 160713, 2023.

6. Namdaria P, Negahdarib B, Eatemadi A, Synthesis, properties and biomedical applications of carbon-based quantum dots: An updated review, Biomedicine & Pharmacotherapy, 87, 209–222, 2017.

7. Khan M E, Mohammad A, Yoon T, State-of-the-art developments in carbon quantum dots (CQDs): Photo-catalysis, bio-imaging, and bio-sensing applications, Chemosphere, 302, 134815, 2022.

8. Thangaraj B, Solomon P R, Chuangchote S, et al, Biomass-derived Carbon Quantum Dots – A Review Part 1: Preparation and Characterization, ChemBioEng Rev, 8 (4), 265–301, 2021.

9. Gao D G, Cheng Y M, Wang P P, et al, An eco-friendly approach for leather manufacture based on P(POSS-MAA)-aluminum tanning agent combination tannage, Journal of Cleaner Production, 257, 120546, 2020.

10. Gao D G, Li N, Li X J, et al, A green tanning method based on POSS-COONa and zirconium: Achieving cleaner leather production, Progress in Organic Coatings, 183, 107718, 2023.